Specifications

Carbon Steel Hollow Bar is in accordance with EN DIN 1629/1630 and EN DIN 2448.

Chemical Composition (%)

Carbon Steel Hollow Bar is supplied in two grades. Grade 20MnVS6 (WNr 1.5217) for sizes 32-250mm and grade St52.0 (WNr 1.0421) for all sizes 250-457mm.

| Grade | C | Si | Mn | P | S | V |
| --- | --- | --- | --- | --- | --- | --- |
| 20MnVS6 | 0.16 - 0.22 | 0.10 - 0.50 | 1.30 - 1.70 | 0.035 max | 0.020 - 0.035 | 0.10 - 0.20* |
| St52.0 | 0.22 max | 0.10 - 0.55 | 1.20 - 1.60 | 0.035 max | 0.020 - 0.035 |  |
| * In addition, steel may contain Nb, whereby V+Nb = max. 0.21% applies. |  |  |  |  |  |  |

20MnVS6 is a micro-alloy steel with improved mechanical properties and with controlled sulphur content to improve machinability. St52.0 is a plain carbon steel defined by its mechanical properties; again, controlled sulphur addition improves machinability.

Mechanical Properties

| Grade | Delivery Condition | Tensile Strength Rm in MPa for wall thickness in mm |  |  | Yield Strength ReH in MPa min. for wall thickness in mm |  |  |  |  | Elongation A in % min. |  | Impact Value ISO-V (long) min. |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | <25 | 25-50 | 50-80 | <12 | 12-25 | 25-40 | 40-50 | 50-65 | long | transv | Test T | J min |
| 20MnVS6 | Untreated | 650-800 | 620-770 |  | 470 | 470 | 450 | 430 |  | 17 | 15 | 0°C | 27 |
|  | Q&T | 700-850 | 650-800 | 520-670 | 590 | 570 | 540 | 510 | 480 | 16 | 14 | -40°C | 27 |
|  |  | <16 | 16-40 | 40-65 | <16 | 16-40 | 40-65 |  |  |  |  |  |  |
| St52.0 | Untreated | 490-630 |  |  | 355 | 345 | 335 |  |  | 17 | 15 | 0°C | 27 |

Heat Treatment

20MnVS6 is suitable for normalising, stress relief and hardening (Q&T). 20MnVS6 can be case hardened (or carbonitrided) to give a case depth of up to 1mm and hardness of up to 60 HRC. For further details consult a heat treatment specialist.

St52.0 is suitable for normalising and stress relieving. For further details consult a heat treatment specialist.

Welding

20MnVS6 hollow bar can be readily welded using all conventional methods. Welds should be completed without interruption. For fillet welds, a multi-pass technique should be selected. Stress relieving is generally not necessary. In case of WT>12mm preheating to 150-200°C is recommended. St52.0 hollow bar can be readily welded using manual and automatic methods. Preheating and/or stress relieving are generally not required, though may be necessary in the case of WT >30mm. For 20MnVS6 and St52.0 basic welding consumables are recommended.

For information on welding at low temperature and other special conditions please consult your local welding specialist.

| Nominal Size |  | Ave Weight | Clean turned sizes OD centered |  | Cleaned turned sizes ID centered |  |  | Nominal Size |  | Ave Weight | Clean turned sizes OD centered |  | Cleaned turned sizes ID centered |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| OD mm | ID mm | kg/m | OD mm | ID mm | OD mm | ID mm |  | OD mm | ID mm | kg/m | OD mm | ID mm | OD mm | ID mm |
| 32 | 20 | 4.2 | 31.5 | 21.9 | 30.5 | 21.4 |  | 90 | 67 | 23.8 | 89.3 | 69.5 | 87.7 | 68.7 |
| 32 | 16 | 5.0 | 31.5 | 18.2 | 30.2 | 17.4 |  | 90 | 63 | 27.0 | 89.3 | 65.8 | 87.7 | 64.8 |
| 36 | 25 | 4.5 | 35.6 | 26.9 | 34.5 | 26.4 |  | 90 | 56 | 32.0 | 89.3 | 59.3 | 87.7 | 58.3 |
| 36 | 20 | 5.9 | 35.6 | 22.3 | 34.1 | 21.5 |  | 90 | 50 | 35.8 | 89.3 | 53.0 | 87.7 | 52 |
| 36 | 16 | 6.7 | 35.6 | 18.6 | 33.9 | 17.4 |  | 95 | 75 | 22.9 | 94.4 | 77.5 | 92.7 | 76.7 |
| 40 | 28 | 5.5 | 39.6 | 30.0 | 38.5 | 29.5 |  | 95 | 67 | 29.6 | 94.4 | 70.0 | 92.4 | 69 |
| 40 | 25 | 6.4 | 39.6 | 27.2 | 38.3 | 26.6 |  | 95 | 56 | 37.9 | 94.4 | 59.0 | 92.1 | 58 |
| 40 | 20 | 7.8 | 39.6 | 23.7 | 38.1 | 21.6 |  | 95 | 50 | 41.7 | 94.4 | 53.5 | 91.9 | 53.3 |
| 45 | 32 | 6.7 | 44.6 | 34.0 | 43.5 | 33.5 |  | 100 | 80 | 25.0 | 100 | 82.5 | 98.2 | 81.6 |
| 45 | 28 | 8.1 | 44.6 | 30.2 | 43.5 | 33.5 |  | 100 | 75 | 29.7 | 100 | 77.7 | 98.1 | 76.8 |
| 45 | 20 | 10.4 | 44.6 | 23.9 | 43.1 | 21.7 |  | 100 | 71 | 33.3 | 100 | 73.8 | 98 | 72.8 |
| 50 | 36 | 8.2 | 49.9 | 38.2 | 48.6 | 37.6 |  | 100 | 63 | 39.9 | 99.9 | 66.0 | 97.6 | 65 |
| 50 | 32 | 9.9 | 49.9 | 34.3 | 48.6 | 33.7 |  | 100 | 56 | 44.7 | 99.9 | 59.2 | 97.4 | 58 |
| 50 | 25 | 12.3 | 49.9 | 27.8 | 48.1 | 27 |  | 106 | 85 | 27.1 | 105.5 | 87.4 | 103.8 | 86.6 |
| 56 | 40 | 10.4 | 55.9 | 42.3 | 54.6 | 41.7 |  | 106 | 80 | 32.0 | 105.5 | 82.7 | 103.5 | 81.8 |
| 56 | 36 | 12.2 | 55.9 | 38.5 | 54.4 | 38.7 |  | 106 | 71 | 40.6 | 105.3 | 73.8 | 103.2 | 72.8 |
| 56 | 28 | 15.3 | 55.9 | 30.9 | 54 | 30 |  | 106 | 63 | 46.8 | 105.3 | 66.0 | 103.1 | 64.9 |
| 63 | 50 | 9.9 | 62.4 | 52.0 | 61 | 51.4 |  | 106 | 56 | 51.7 | 105.3 | 59.3 | 103 | 58 |
| 63 | 45 | 12.8 | 62.4 | 47.2 | 60.9 | 46.5 |  | 112 | 90 | 29.9 | 111.3 | 92.4 | 109.6 | 91.6 |
| 63 | 40 | 15.3 | 62.4 | 41.4 | 60.7 | 40.6 |  | 112 | 80 | 40.3 | 111.3 | 82.7 | 109.3 | 81.7 |
| 63 | 36 | 17.2 | 62.4 | 38.6 | 60.5 | 37.7 |  | 112 | 71 | 48.4 | 111.3 | 74.1 | 109.1 | 73 |
| 63 | 32 | 18.8 | 62.4 | 34.7 | 60.4 | 33.8 |  | 112 | 63 | 54.9 | 111.3 | 66.2 | 108.9 | 65 |
| 71 | 50 | 16.6 | 70.3 | 52.6 | 68.6 | 51.8 |  | 118 | 90 | 38.5 | 117.2 | 93.0 | 115.1 | 92 |
| 71 | 45 | 19.5 | 70.3 | 47.9 | 68.4 | 47 |  | 118 | 80 | 48.9 | 117.2 | 83.1 | 114.5 | 82.1 |
| 71 | 40 | 22.1 | 70.3 | 43.0 | 68.5 | 42 |  | 118 | 71 | 57.2 | 117.2 | 74.2 | 114.4 | 73 |
| 71 | 36 | 24.0 | 70.3 | 39.1 | 68.4 | 38 |  | 118 | 63 | 63.7 | 117.2 | 66.3 | 114.3 | 64.9 |
| 75 | 56 | 16.7 | 74.7 | 58.5 | 73.1 | 57.5 |  | 125 | 100 | 37.8 | 124.3 | 102.9 | 122.4 | 102 |
| 75 | 50 | 20.5 | 74.7 | 53.0 | 72.9 | 52.1 |  | 125 | 95 | 43.8 | 124.3 | 97.9 | 122.3 | 96.9 |
| 75 | 45 | 23.6 | 74.7 | 48.2 | 72.8 | 47.2 |  | 125 | 90 | 49.8 | 124.3 | 92.9 | 122.2 | 91.9 |
| 75 | 40 | 26.2 | 74.7 | 43.2 | 72.7 | 42.2 |  | 125 | 80 | 59.6 | 124.3 | 83.3 | 121.9 | 82.1 |
| 80 | 63 | 16.2 | 79.4 | 65.4 | 77.9 | 64.7 |  | 125 | 71 | 67.9 | 124.3 | 74.7 | 121.6 | 73.3 |
| 80 | 56 | 21.3 | 79.4 | 58.7 | 77.6 | 57.8 |  | 132 | 106 | 41.3 | 130.9 | 108.8 | 128.9 | 107.8 |
| 80 | 50 | 25.2 | 79.4 | 52.9 | 77.4 | 51.9 |  | 132 | 98 | 51.8 | 130.9 | 100.6 | 128.8 | 99.6 |
| 80 | 45 | 28.3 | 79.4 | 47.9 | 77.4 | 46.9 |  | 132 | 90 | 60.2 | 130.9 | 93.0 | 128.7 | 91.9 |
| 80 | 40 | 30.7 | 79.4 | 42.9 | 77.3 | 41.9 |  | 132 | 80 | 70.6 | 130.9 | 83.6 | 128.1 | 82.3 |
| 85 | 67 | 18.2 | 84.5 | 69.5 | 83 | 68.8 |  | 132 | 71 | 78.8 | 130.9 | 74.9 | 127.7 | 73.4 |
| 85 | 55 | 27.2 | 84.5 | 58.0 | 82.5 | 57 |  | 140 | 112 | 47.5 | 138.9 | 114.8 | 136.9 | 113.8 |
| 85 | 45 | 33.1 | 84.5 | 48.0 | 82 | 47 |  | 140 | 106 | 55.8 | 138.9 | 109.0 | 136.8 | 108 |
| 90 | 71 | 20.5 | 89.3 | 73.4 | 87.7 | 72.6 |  | 140 | 100 | 62.8 | 138.9 | 103.5 | 136.7 | 102.4 |
| Nominal Size |  | Ave Weight | Clean turned sizes OD centered |  | Cleaned turned sizes ID centered |  |  | Nominal Size |  | Ave Weight | Clean turned sizes OD centered |  | Cleaned turned sizes ID centered |  |
| OD mm | ID mm | kg/m | OD mm | ID mm | OD mm | ID mm |  | OD mm | ID mm | kg/m | OD mm | ID mm | OD mm | ID mm |
| 140 | 90 | 74.4 | 138.9 | 93.7 | 136.3 | 92.4 |  | 212 | 150 | 146.6 | 210 | 154.9 | 207.1 | 152 |
| 140 | 80 | 84.7 | 138.9 | 84.0 | 135.9 | 82.4 |  | 212 | 125 | 189.0 | 210 | 130.2 | 206.6 | 126.7 |
| 150 | 125 | 47.2 | 149 | 127.6 | 147.2 | 126.7 |  | 224 | 180 | 119.0 | 222.3 | 184.9 | 219.9 | 182.5 |
| 150 | 118 | 57.3 | 149 | 121.2 | 146.8 | 102.1 |  | 224 | 160 | 160.7 | 222.3 | 165.6 | 219.3 | 162.5 |
| 150 | 106 | 73.6 | 149 | 109.4 | 146.6 | 108.2 |  | 224 | 132 | 210.2 | 221 | 138.8 | 216.2 | 134 |
| 150 | 95 | 87.1 | 149 | 98.6 | 146.6 | 97.1 |  | 236 | 190 | 132.0 | 232 | 196.5 | 228.5 | 193 |
| 150 | 80 | 103.0 | 149.3 | 83.9 | 146.4 | 81 |  | 236 | 170 | 176.0 | 232 | 176.9 | 228.1 | 173 |
| 160 | 132 | 56.5 | 159.1 | 134.6 | 146.4 | 133.8 |  | 236 | 140 | 231.9 | 232 | 150.2 | 224.8 | 143 |
| 160 | 122 | 71.0 | 159.1 | 124.6 | 146.4 | 123.6 |  | 250 | 200 | 152.5 | 246 | 208 | 241 | 203 |
| 160 | 112 | 85.3 | 159.1 | 115.6 | 157.1 | 114.4 |  | 250 | 180 | 197.5 | 246 | 189 | 240 | 183 |
| 160 | 100 | 101.0 | 159.1 | 104.4 | 155.8 | 102.8 |  | 250 | 200 | 257.1 | 246 | 161 | 238 | 153 |
| 160 | 90 | 112.0 | 159.1 | 94.2 | 155.9 | 91 |  | 273 | 180 | 153.0 | 269 | 232 | 265 | 227 |
| 162 | 111 | 85.6 | 160 | 115.0 | 157.5 | 114.4 |  | 273 | 150 | 180.0 | 269 | 223 | 264 | 218 |
| 162 | 79 | 122.8 | 160 | 85.0 | 155.9 | 94 |  | 273 | 223 | 210.0 | 269 | 212 | 263 | 206 |
| 170 | 140 | 64.2 | 169.1 | 142.9 | 167 | 142 |  | 273 | 213 | 230.0 | 269 | 205 | 263 | 198 |
| 170 | 130 | 79.6 | 169.1 | 133.0 | 166.9 | 132.1 |  | 273 | 201 | 275.0 | 269 | 187 | 261 | 179 |
| 170 | 118 | 97.8 | 169.1 | 121.8 | 166.3 | 120.6 |  | 298 | 193 | 137.0 | 294 | 266 | 291 | 262 |
| 170 | 100 | 122.0 | 169.2 | 104.4 | 166 | 101.2 |  | 298 | 173 | 199.0 | 294 | 248 | 289 | 243 |
| 180 | 150 | 68.7 | 179.2 | 152.9 | 177.1 | 152 |  | 298 | 258 | 255.0 | 294 | 230 | 288 | 223 |
| 180 | 140 | 85.3 | 179.2 | 142.9 | 177 | 142.1 |  | 298 | 238 | 306.0 | 294 | 212 | 286 | 204 |
| 180 | 125 | 109.9 | 179.2 | 128.9 | 176.2 | 127.6 |  | 324 | 218 | 184.0 | 319 | 283 | 316 | 279 |
| 180 | 100 | 144.0 | 179.3 | 104.5 | 175.8 | 101 |  | 324 | 198 | 280.0 | 319 | 256 | 313 | 249 |
| 190 | 160 | 73.7 | 189.4 | 164.0 | 187.4 | 162 |  | 324 | 274 | 338.0 | 319 | 238 | 312 | 230 |
| 190 | 150 | 90.7 | 189.4 | 154.7 | 187.2 | 152 |  | 356 | 306 | 204.0 | 351 | 315 | 347 | 311 |
| 190 | 132 | 122.0 | 189.4 | 136.6 | 186.5 | 133.7 |  | 356 | 276 | 311.0 | 351 | 288 | 345 | 282 |
| 190 | 118 | 143.0 | 189.4 | 122.6 | 186.2 | 119.4 |  | 356 | 256 | 377.0 | 351 | 270 | 343 | 262 |
| 190 | 106 | 160.0 | 189.4 | 110.3 | 186.1 | 107 |  | 356 | 236 | 438.0 | 351 | 252 | 342 | 243 |
| 200 | 160 | 96.9 | 198 | 164.4 | 195.6 | 162 |  | 406 | 306 | 439.0 | 400 | 320 | 393 | 312 |
| 200 | 140 | 133.0 | 198 | 144.9 | 195.1 | 142 |  | 406 | 286 | 512.0 | 400 | 302 | 391 | 293 |
| 200 | 112 | 176.0 | 198 | 116.9 | 194.6 | 113.7 |  | 419 | 319 | 455.0 | 413 | 333 | 406 | 325 |
| 212 | 170 | 108.0 | 210 | 174.9 | 207.6 | 172.5 |  |  |  |  |  |  |  |  |

Figures based on EN DIN 1629/1630 and EN DIN 2248 and mill information. Clean turned sizes 250mm and over indicative figures only. Clean turned sizes are valid for parts with length up to 120mm. Due to out-of-straightness tolerance for longer parts 2mm/1000mm must be deducted from OD figures and added to ID figures.

Limitation of Liability The information contained in this Atlas Steels Carbon Steel Hollow Bar Grade Data Sheet document is not an exhaustive statement of all relevant information. It is a general guide for customers to the products and services available from Atlas Steels and no representation is made or warranty given in relation to this information or the products or processes it describes.