Grade 12L14FM

Grade 12L14FM is a free machining carbon steel bar containing maximum 0.15% Carbon. Due to the addition of Lead (Pb) this grade has the highest machinability and is suitable for high-volume ultra-high-speed machining.

Related Specifications

Free machining bar grade 12L14FM is supplied as per one of the following alternative standards:

- AS1443 grade 12L14, ASTM A108 grade 12L14.

- ASTM A108 grade 1213 or grade 1215.

- Euronorm EN 10087 grade 11SMnPb37 (1.0737).

Chemical Composition (%)

| Grade | C | Si | Mn | P | S | Pb |
| --- | --- | --- | --- | --- | --- | --- |
| 12L14 | ≤ 0.15 | ≤ 0.10 | 0.80 - 1.20 | 0.04 - 0.09 | 0.25 - 0.35 | 0.15 - 0.35 |
| 11SMnPb37 | ≤ 0.14 | ≤ 0.05 | 1.00 - 1.50 | ≤ 0.11 | 0.34 - 0.40 | 0.20 - 0.35 |

The grades are equally characterised by very high and consistent machinability and the ability to be electroplated. Grades can be interchanged without problems and no marked changes in machinability are to be expected.

Conditions of Supply – Typical Mechanical Properties

Grade 12L14FM is not guaranteed to meet any specified minimum tensile property requirements. The values in the table below reflect typical properties only. These mechanical properties (except for HB values) are specified in AS1443 grade D13 (cold drawn) and AS1443 grade T13 (peeled and polished).  Grade D13 and T13 are essentially grade 12L14FM with guaranteed mechanical properties.

| Condition | Diameter (mm) | Tensile Strength (MPa) | Yield Stress (MPa) | Elongation (% in 50mm) | Hardness (HB) |
| --- | --- | --- | --- | --- | --- |
| Cold Drawn | Up to 16mm inclusive | 480 min | 350 min | 7 min | 142 - 226 |
|  | >16mm to 38mm inclusive | 430 min | 330 min | 8 min | 126 - 210 |
|  | >38mm to 100mm inclusive | 400 min | 290 min | 9 min | 119 - 200 |
| Cold Finished / Turned and Polished | To 260mm inclusive | 370 min | 230 min | 17 min | 105 - 154 |

Grade 12L14FM can be supplied with guaranteed mechanical properties on special order request.

Conditions of Supply – Finish, Dimensions and Tolerances

Surface Finish

Bright round bar up to 63.5mm diameter is all cold drawn. Bright round bar 63.5-100mm diameter are cold drawn or smooth-turned and polished. Bright round bars over 100mm diameter are all smooth-turned and polished.

All hexagon bar and all square are cold drawn. Flat bar is cold drawn and supplied sharp-edge.

Diameter and A/F Tolerances

Round Bar: Drawn h10; Smooth-turned and polished h10 or h11.

Square, Flat & Hexagon Bar:	h11.

Straightness – Maximum Deviation from a Straight Line

Round Bar:	1 in 1000mm.

Square, Flat & Hexagon Bar:	1 in 375mm.

Other tolerances may be supplied for more critical applications upon enquiry.

Length Tolerance Bright Bar

Mill Lengths (3.5 to 6.0m): ± 250mm max.

Set Lengths (3.0 to 7.0m): -0/+40mm max. tolerance is possible subject to enquiry.

Welding

Grade 12L14FM is not suitable for any welding. Lead fumes originating during the welding operation constitute a health hazard.

Applications of Grade 1214FM

General repetition engineering applications where the lower strength of this product is acceptable. Grade 12L14FM is not capable of being through hardened and is not hardenable by either flame or induction hardening processes. It can be case hardened by a blank carburising process. Applications such as domestic bin axles, concrete anchors, padlock shackles (case hardened), hydraulic fittings, vice jaws (case hardened). Ductility of grade 12L14FM is low, so it is not suitable for applications requiring significant bending or forming.

Possible Alternative Grades

| Grade | Why it might be chosen instead of 12L14FM |
| --- | --- |
| 1214FM | Slightly lower machinability than 12L14FM. Recommended in case the use of leaded steels is a factor of concern, such as in welding or general environmental concern. |
| M1020 | Where welding is required, and machinability is a secondary requirement. Also, where the finally machined components are to be electroplated and a better quality plated finish is a requirement. Where higher ductility is required because of significant bending and forming. |
| M1030 | Where higher strength is required, and welding and bending may be required. Pre-and post-heat may be required as part of the welding procedure, whereas M1020 is readily welded without pre-& post heating. |
| Limitation of Liability The information contained in this Atlas Steels Free Machining Steel Bright Carbon Bar 12L14FM Grade Data Sheet document is not an exhaustive statement of all relevant information. It is a general guide for customers to the products and services available from Atlas Steels and no representation is made or warranty given in relation to this information or the products or processes it describes. |  |